## Slide 1: Pressure Dependence of Superconductivity of Iron Chalcogenides
Shimizu group
M1 Hidenori Fujita

## Slide 2
Contents
Introduction
  High pressure
  Superconductor
  KxFe2-ySe2
My experiment
  High pressure experiment
  Sample & Data
Conclusion & Future work

## Slide 3
introduction
High Pressure
  1 GPa = 10,000 atm
    ≅ 100,000 m (water depth)
  360 GPa ≅ center of the earth
http://www.jsanet.or.jp/qanda/text/q1_03.html
100,000m
http://www.spring8.or.jp/ja/news_publications/research_highlights/no_57/

## Slide 4
introduction
High Pressure
  Pressure can change crystal structure
    atomic distance, structure type ….. etc.
Molecule
Insulator
pressurization
pressurization
monatomic metal
(金属単原子)

## Slide 5
Introduction
Superconductivity (SC)超伝導
  Zero resistance
  Meissner effect
  Emerge at low temperature
  Application
    Superconducting magnet
    SQUID
    Transmission line
    …. etc.
http://www.st-h.ed.jp/oldpage/club-page/kaken/physics/katudou/tyoudenndou.html
http://www.kek.jp/ja/NewsRoom/Highlights/20110512133324/

## Slide 6
Introduction
Pressure dependence of SC
  Transition temperature can change with pressure
http://www.jst.go.jp/pr/announce/20080424/
Journal of the Physical Society of Japan
Vol. 78, No. 6, June, 2009, 063705

## Slide 7
Introduction
History of Tc
  Highest ≅ 170 K (under high pressure in HgBa2Ca2Cu3O8+δ(Hg-1223) )
  Iron based superconductor
    Tc < 60 K
    Chalcogenide & pnictide

## Slide 8
Introduction
KxFe2-ySe2
  Tc of KxFe2-ySe2 decrease by applying pressure
  SC phase re-emerge at higher pressure (at 11GPa)
doi:10.1038/nature10813

## Slide 9
Motivation
Research….
  difference of sample (amount of K)
    Previous research : K0.8Fe1.7Se2
  behavior at high pressure

## Slide 10
My experiment
  High pressure experiment
  Apply pressure with Diamond Anvil Cell

## Slide 11
My experiment
  High pressure experiment
  How to measure the electrical resistance

## Slide 12
My experiment
Sample 1
  Property and condition
Run 1
Run 2
K0.66Fe1.78Se2
(amount of K is few)

## Slide 13
My experiment
Sample 1
  Results
Run 1
Run 2

## Slide 14
My experiment
Sample 1
  Results
Notes: 10GPa~の拡大
今回の測定では転移温度の減少は確認できましたがSC2-phaseの確認はできませんでした。こちらは10GPa以降の電気抵抗の様子ですが、先行研究のようなドロップは見られていません。

## Slide 15
My experiment
Sample 2
  Property and condition
K0.8Fe2Se2
(original composition)

## Slide 16
My experiment
Sample 2
  Results

## Slide 17
My experiment
Sample 1
  Results

## Slide 18
Sample 1
Sample 2

## Slide 19
Conclusion & Future work
SC1-phase remains
  SC2-phase didn’t appear
Future work
  Change the amount of Fe
  Continue to research at high pressure