## Slide 1
Measurement of nano-scale physical characteristics in VO2
nano-wires by using Scanning Probe Microscope (SPM)
Tanaka lab.
Kotaro Sakai
a VO2 nano-wire

## Slide 2
Contents
・Background
Strongly correlated electron system
The characteristics of VO2
VO2 nano-wire
・My work
Purpose of my research
Fabrication of VO2 nano-wires
SEM & AFM images of VO2 nano-wires
・Summary
・Future work

## Slide 3
Strongly correlated electron system
Band Width : wide
Band Width : narrow
Partial occupation ⇒
Metal
Partial occupation ⇒ but Insulator
Coulomb's repulsion U
Hubbard model
Band Width：
S band > P band > d band > f band
3d > 4d > 5d

## Slide 4
Strongly correlated electron system
Insulator
Metal
Stimulation
Temperature
Electric field
Strain

## Slide 5
Vanadium dioxide (VO2) has attractive properties as follows:
1. Orders of magnitude resistive changes due to a metal-insulator transition (MIT)
2. Coexistence of metallic and insulating domains with several tens nanometer in size during MIT.
The characteristics of VO2
High-T: metal
Low-T: insulator

## Slide 6
VO2 nano-wire
・Step resistivity changes in VO2 micro-wires and nano-wires(200nm)
Phys. Rev. Lett 101, 1750 (2008)
Appl. Phys. Lett. 104, 023104 (2014)
These data show MIT in VO2 domains is first order phase transition.
・VO2 nano-wire (<50nm) makes large and sharp resistivity change.
・Each nano-scale domain conductive behavior is clearly appeared.
・The electron conducting path is simplified.
The advantage of VO2 nano-wire

## Slide 7
The characteristics of VO2
・Transmittance(透過率)
・Work function(仕事関数)
Appl. Phys. Lett. 101, 191605 (2012)
Insulator
Metal + Insulator
Metal
・Seebeck coefficient(ゼーベック係数)
Nano Lett. 9, 4001(2009)
・Carrier density(キャリア密度)
Phys. Rev. B 79, 153107 (2009)
Appl. Phys. Lett. 102, 153106(2013)

## Slide 8
My purpose
Fabrication of VO2 nano-wire which width is
smaller than domain size (approximately 50nm)
and Measurement of these physical properties

## Slide 9
Fabrication of VO2 nano-wires
Chemical Vapor Deposition(CVD,化学気相合成法)
50μm
w=～30nm(the upper inset)
w=50～100nm
They successfully fabricated VO2 nano-wires which width
is under 50nm,but didn‘t report these electrical properties.
・Conventional method

## Slide 10
Fabrication of VO2 nano-wires
Resist
mold
2, Nano-imprinting
Target
pulsed laser
substrate
VO2
1, Deposition
4, Resist removal
a VO2 nano-wire
3, Etching(RIE)
O2,SF6plasma
・Our fabrication method
Combination of Pulsed Laser Deposition (PLD) and
Nano-Imprint Lithograph (NIL) techniques
UV

## Slide 11
Chemical Vapor Deposition
Sung-Hwan Bae et al, Adv. Mater, 25, 5098 (2013)
Pulsed Laser Deposition (PLD)
& Nano Imprint Lithography (NIL)
Position : uncontrollable
Making devices : difficult
Position : precisely controllable
Making devices : easy
Conventional method
Our method
electrode
50μm
Fabrication of VO2 nano-wires

## Slide 12
SEM images of VO2 nano-wires
Space between wires : 138nm
Wire thickness : 20nm
Wire width : 22nm
Space between wires : 195nm
Wire thickness : 20nm
Wire width : 45nm
We successfully fabricated VO2 nano-wires which
width is smaller than domain size.
・SEM images
a VO2 nano-wire
a VO2 nano-wire
120nm_nano-wires pattern
80nm_nano-wires pattern

## Slide 13
Measurement system
Pt electrode
Al2O3
VO2-NW
A cantilever coated with Pt
Pt electrode
The advantage of this method is we can freely select distance between electrodes.
・Conductive-AFM

## Slide 14
a difference between SEM and AFM images
80nm nano-wires pattern(line and space : 1:1)
VO2 nano-wire
SEM image
AFM image
65nm

## Slide 15
C-AFM images of VO2 nano-wires (at Room Temperature)

## Slide 16
Resistivity of VO2 nano-wires (at Room Temperature)
This VO2 nano-wire | Typical VO2 thin film
0.54[Ωcm] | 0.1～1.0[Ωcm]
Al2O3
VO2-NW
A cantilever coated with Pt
Pt electrode
Rsystem
Rcontact
Rsample

## Slide 17
RT(+300mV)
150nA
500nm
360K(+20mV)
500nm
Distance[μm]
Current[nA]
 | RT | 360K
Resistivity | 0.54[Ωcm] | ＜0.005[Ωcm]
Insulator-Metal Transition

## Slide 18
Summary
We successfully fabricated VO2 nano-wires with
approximately 20 nm in width , which is smaller than
domain size.
We observed the electric current in VO2 nano-wires with
by using C-AFM and could estimate the resistivity of the
VO2 nano-wire, which is consistent value with typical VO2.
RT(+300mV)
500nm
360K(+20mV)
500nm

## Slide 19
Future work
・We will observe huge resistive
change during MIT which is
characteristics of VO nano-wires .
・We will observe one domain behavior
and investigate the relationship
between nano-domain spatial address
and a conductive property.
Appl. Phys. Lett. 104, 023104 (2014)