## Slide 1: Magnetism and Superconductivity of Copper-Oxide Superconductor
Kitaoka Lab.
Nozomu Shiki
T.ADACHI et al., J. Phys. Soc. Jpn. 82 (2013) 063713
Y.Krockenberger et al., Scientific Reports Volume: 3, Article number: 2235

## Slide 2: Contents
Introduction
History of Superconductivity
Main subject
Copper-Oxide Superconductor
(Hole and electron doping type)
Pr2-xCexCuO4(thin film)
Summary

## Slide 3: History of Superconductivity
年
1910
1930
1950
1970
1990
liquid nitrogen
Pb
Nb
NbC
NbN
Nb3Sn
V3Si
Nb3Ge
Nb-Al-Ge
LaBaCuO
LaSrCuO
YBaCuO
BiCaSrCuO
TlCaBaCuO
HgCaBaCuO
TlCaBaCuO
HgCaBaCuO
（under high pressure）
HgCaBaCuO
（under high pressure）
0
60
80
100
160
1986
Tc (K)
100
160
1911
O
Hg
High-Tc copper oxides
Introduction

## Slide 4: kind of carriers (Electrons, Holes）
La (Sr)
La2-ｘSrxCuO4
La3+ Sr2+
Hole type (T-structure)
Cu
T
x
La2-xSrxCuO4
Nd2-xCexCuO4
AFM
SC
0
0.15
0.15
Nd
3+
→
Ce
4+
La
3+
→
Sr
2+
Hole doping
Electron doping
SC
Mother material is Mott insulator.
x
Notes: キャリアが増えるにつれて

## Slide 5: kind of carriers (Electrons, Holes）
La (Sr)
La2-ｘSrxCuO4
La3+ Sr2+
Hole type (T-structure)
Cu
T
x
La2-xSrxCuO4
Nd2-xCexCuO4
AFM
SC
0
0.15
0.15
Nd
3+
→
Ce
4+
La
3+
→
Sr
2+
SC
Mother material is Mott insulator.
x
Hole doping
Electron doping
Notes: キャリアが増えるにつれて

## Slide 6
La2CuO4
Mott Insulator
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d9)
High-Tc Superconductor
Notes: La2CuO4

## Slide 7
Cu2+ (3d9)
La2CuO4
Mott Insulator
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
x2-y2
3z2-r2
yz
zx
xy
Crystal field
Cu2+
O2-
O2-
O2-
O2-
O2-
O2-
cubic symmetry
High-Tc Superconductor
Notes: La2CuO4

## Slide 8
ＣｕＯ２plane
Cu2+ (3d9)
Charge Reservoir
Charge Reservoir
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2CuO4
Mott Insulator
O2-
Cu2+
O2-
O2-
O2-
O2-
O2-
Jahn-Teller effect
Crystal field
High-Tc Superconductor
Notes: La2CuO4

## Slide 9
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d9)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2CuO4
Mott Insulator
Jahn-Teller effect
Crystal field
High-Tc Superconductor
Antiferromagnetic interaction Ｊ
t
U: coulomb energy
t : hopping energy
Notes: 反強磁性ならパウリ排他より飛び移って戻るというのが許されエネルギー的に得

## Slide 10
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d9)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2CuO4
Mott Insulator
Jahn-Teller effect
Crystal field
High-Tc Superconductor
Antiferromagnetic interaction Ｊ
U
t
U: coulomb energy
t : hopping energy
Notes: 反強磁性ならパウリ排他より飛び移って戻るというのが許されエネルギー的に得

## Slide 11
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d9)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2CuO4
Mott Insulator
Jahn-Teller effect
Crystal field
High-Tc Superconductor
Antiferromagnetic interaction Ｊ
U: coulomb energy
t : hopping energy
U
t
Notes: 反強磁性ならパウリ排他より飛び移って戻るというのが許されエネルギー的に得

## Slide 12
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
La2CuO4
Mott Insulator
x2-y2
3z2-r2
yz
zx
xy
Jahn-Teller effect
High-Tc Superconductor
DOS
E
U.H.B.
L.H.B.
Notes: 反強磁性ならパウリ排他より飛び移って戻るというのが許されエネルギー的に得

## Slide 13
La2CuO4
Mott Insulator
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
High-Tc Superconductor
U:Mott Hubbard gap
Δ:charge transfer gap
!!
Δ
U
E
EF
Notes: 反強磁性ならパウリ排他より飛び移って戻るというのが許されエネルギー的に得

## Slide 14
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d9)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2-xSrxCuO4
Sr2+
La3+
substitution
Sr2+
High-Tc Superconductor
E
EF
T
La2-xSrxCuO4
Nd2-xCexCuO4
AFM
SC
Nd
3+
→
Ce
4+
La
3+
→
Sr
2+
Hole doping
Electron doping
SC
x
Notes: La2CuO4

## Slide 15
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d9)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2-xSrxCuO4
Sr2+
La3+
substitution
Sr2+
High-Tc Superconductor
E
EF
Notes: La2CuO4

## Slide 16
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d9)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2-xSrxCuO4
Sr2+
La3+
substitution
Sr2+
High-Tc Superconductor
E
EF
Hole

## Slide 17
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d9)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2-xSrxCuO4
EF
Sr2+
La3+
substitution
Sr2+
High-Tc Superconductor
E
Hole
S=0

## Slide 18
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d8)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2-xSrxCuO4
Sr2+
La3+
substitution
Sr2+
High-Tc Superconductor
E
EF
Hole
S=0

## Slide 19
ＣｕＯ２plane
Charge Reservoir
Charge Reservoir
Cu2+ (3d8)
x2-y2
3z2-r2
yz
zx
xy
x2-y2
3z2-r2
yz
zx
xy
La2-xSrxCuO4
Sr2+
La3+
substitution
Sr2+
High-Tc Superconductor

## Slide 20: Hole doping
La (Sr)
La2-ｘSrxCuO4
La3+ Sr2+
As carriers increase, the groundstate changes from AFM to SC.
Hole doping type
(T-structure)
Cu
T
x
AFM
SC
0
0.15
0.15
SC
Mother material is Mott insulator.
La2-xSrxCuO4
La3+
Sr2+
Hole doping
Nd2-xCexCuO4
Nd3+
Ce4+
Electron doping
→
→
Cu
O
La,
Sr
Notes: キャリアが増えるにつれて

## Slide 21: Electron doping
Nd (Ce)
Cu
Nd2-ｘCeｘCuO4
Nd3+ Ce4+
Electron doping type
(T’-structure)
T
x
AFM
SC
0
0.15
0.15
SC
Mother material is Mott insulator.
La2-xSrxCuO4
La3+
Sr2+
Hole doping
Nd2-xCexCuO4
Nd3+
Ce4+
Electron doping
→
→
Cu
O
Nd,
Ce
As carriers increase, the groundstate changes from AFM to SC.
Notes: キャリアが増えるにつれて

## Slide 22: Electron doping
Nd2-ｘCeｘCuO4
Nd3+ Ce4+
Electron doping type
(T’-structure)
Nd (Ce)
Cu
EF
EF
x2-y2
3z2-r2
yz
zx
xy
Cu2+ (3d9)
doping
Notes: キャリアが増えるにつれて

## Slide 23: Electron doping
Nd2-ｘCeｘCuO4
Nd3+ Ce4+
Electron doping type
(T’-structure)
Nd (Ce)
EF
x2-y2
3z2-r2
yz
zx
xy
Cu2+ (3d10)
doping
Cu
EF
Notes: キャリアが増えるにつれて

## Slide 24: Electron doping
Nd2-ｘCeｘCuO4
Nd3+ Ce4+
Electron doping type
(T’-structure)
Nd (Ce)
EF
x2-y2
3z2-r2
yz
zx
xy
Cu2+ (3d10)
doping
Cu
EF
Notes: キャリアが増えるにつれて

## Slide 25: Electron doping
Nd2-ｘCeｘCuO4
Nd3+ Ce4+
Electron doping type
(T’-structure)
Nd (Ce)
EF
x2-y2
3z2-r2
yz
zx
xy
Cu2+ (3d10)
doping
Cu
EF
Notes: キャリアが増えるにつれて

## Slide 26
Pr2-xCexCuO4 (thin film)
annealing
(10-6 Torr , 550K)
annealing(1st)
(10-1 Torr , 800K)
annealing(2nd)
(10-6 Torr , 550K)
AFM
SC
http://infrared.phy.bnl.gov/pdf/homes/homes_02.pdf
Pr2CuO4

## Slide 27
2 step annealing
Pr2CuO4
as grown

## Slide 28
O
Pr2CuO4+δ
Pr2CuO4+δ
http://infrared.phy.bnl.gov/pdf/homes/homes_02.pdf
as grown
2 step annealing
Notes: では、なぜ酸素を除去することによって超伝導が発現するのか、ということを理解するために、新しい電子・磁気状態が提案されています。

## Slide 29
influence of excess oxygen
E
E
EF
U
EF
Cu
O
Cu-O bond becomes longer
Cu
O

## Slide 30
E
E
EF
EF
U
O
influence of excess oxygen
Cu-O bond becomes longer
Cu
Cu
O

## Slide 31
E
EF
EF
U
E
O
influence of excess oxygen
Cu
Cu
Cu-O bond becomes longer
O

## Slide 32: Summary
Lattice constant of c-axis decreases by appropriate annealing, and SC appears in Pr2CuO4(thin film),
Length of Cu-O bonds in a square plane is larger than in a pyramidal plane,
because of removing apical oxygen
energy of goes down, and metal states realize in Fermi surface
Cu
O
Cu
O

## Slide 33
END