## Slide 1: Search for liquid-metallic hydrogen under high temperature and high pressure
Shimizu group
M1 SHO Kawaguchi
  V. Dzyabura et al. PNAS, 110, 20, 8040-8044 (2013)
  M. I. Eremets et al. Nat. Mater., 10, 927-931 (2011)

## Slide 2
Contents
Introduction
  About high pressure
  About Hydrogen
previous work
  LASER heating
Future work
  Electric resistance measurement
Conclusion

## Slide 3
About high pressure
High Pressure
  1 GPa ≈ 10,000 atm ≈ 10,000 kgf/cm2
    (Center of the Earth = 360 GPa)
Pressure can change crystal structure
  atomic distance, structure type … etc.
Molecule
Insulator
pressure
pressure
monatomic metal

## Slide 4
About Diamond Anvil Cell
Diamond Anvil Cell
(DAC)
Diamond anvil
gasket
sample
Apply pressure
Why use Diamond? .....
Very hard → high pressure
      (～ 350 GPa)
Transparent → optical measuring
3cm
6cm

## Slide 5
About Hydrogen
Jupiter

## Slide 6
Experiment has NOT been under high temperature and high pressure
Liquid H2
Liquid- metallic H
Observe liquid-metallic hydrogen and
determine phase transition boundary
About Hydrogen

## Slide 7
About Hydrogen
Technical difficulties of experiments
Small atomic radius and high diffusibility (拡散性)
  → Hydrogen embrittlement (水素脆化) of diamond anvil
  and reduction of hydrogen
High compressibility(圧縮率)
  → Contraction of the sample room
Apply pressure
@ 50 GPa
@ 1 atm

## Slide 8
Previous Work
LASER heating ( T vs LASER power )
Heating efficiency changes
Metallized
Specific heat capacity(比熱)
and reflectance changes
LASER power
Temperature
metalized
transition temperature

## Slide 9
LASER heating
Setting
prevent gold from touching with diamond
Anvil Culet : φ100 μm
Gasket : Re
LASER absorber : Pt
Heating LASER : 1065 nm
Heating LASER
Al2O3 coating on the diamond surface
(to prevent hydrogen embrittlement of diamond )
V. Dzyabura et al. PNAS, 110, 20, 8040-8044 (2013)

## Slide 10
LASER heating
V. Dzyabura et al. PNAS, 110, 20, 8040-8044 (2013)
Results
Heating efficiency changes
Catch the metallization of Hydrogen
inflection point

## Slide 11
LASER heating
LASER heating
Ichimaru. K. et al. (2014)
heating
Au foil
Anvil Culet : φ100 or 150 μm
Gasket : Re+NaCl
LASER absorber : Gold
Heating LASER : 1053 nm
(To prevent hydrogenation of Rhenium)

## Slide 12
LASER heating
Ichimaru. K. et al. (2014)
Results
Heating efficiency changes
Catch the metallization of Hydrogen

## Slide 13
LASER heating
Liquid H2
Metallic liquid H
Liquid-metallic hydrogen was observed by LASER heating.

## Slide 14
Future work
In order to confirm the metallization directly….
Electric resistance measurement
  Drop of electric resistance with the metallization
Raman spectroscopy
  Loss of vibron of hydrogen with the metallization

## Slide 15
Resistance measurement
M. I. Eremets et al. Nat. Mater., 10, 927-931 (2011)
Setting
Anvil Culet : φ20 μm
Gasket : Re
Electrodes : Pt
Insulating layer : Alumina+epoxy

## Slide 16
Resistance measurement
M. I. Eremets et al. Nat. Mater., 10, 927-931 (2011)
Drop of resistance
Metallized?
Results
@R.T.
Observe drop of electrical resistance @ 270 GPa
→ Metallized?

## Slide 17
Conclusion
Liquid H2
Metallic liquid H
Liquid-metallic hydrogen was observed by LASER heating.
Electric resistance measurement is needed to confirm the metallization of hydrogen.