## Slide 1: High pressure phase diagram of Beryllium Phys.Rev.B 86,174118(2012)
2014.06.11
Shimizu Lab.
Takuya Yamauchi

## Slide 2: Contents
Introduction
Motivation
Supplements
Experiment
Summary
Future work

## Slide 3: Superconductivity of beryllium Introduction
Fig. Superconducting transition temperature of elements.(under pressure)
Tc: superconducting transition temperature.
Beryllium
Tc=24mK
The value is considerably lower than other light elements.
So Tc may enhance in high pressure?
What causes?
Ref. HP@SPring8(2011)
※Tc: 超伝導転移温度

## Slide 4: Enhancement of Tc Introduction
From BCS theory
Tc ∝
θD: Debye temperature
N: Density of state at the Fermi surface
Tc: superconducting transition temperature.
According to previous presentation...
Applying pressure causes
Structural transition
Electronic states change.
Let’s inspect how the structure of beryllium would change under high pressure!!

## Slide 5: Structure of beryllium Introduction
Beryllium has small c/a ratio.→ 1.568
(Its ideal value of hcp is 1.633 )
hcp(～1530K)
bcc(1530～1560K)
heat
pressure
α-Be(hcp structure) is
stable at ambient temperature and pressure.
β-Be(bcc structure) would be appeared at high temperature and prssure.
Ref. D. A. Young, Phase Diagrams of the Elements (University of California, 1991), P. 79.c

## Slide 6: Motivation
Measuring P-V and c/a of Be to high precision.
Confirming the stability field of β-Be predicted at high pressure.

## Slide 7: Loading of beryllium supplements
Beryllium
Rhenium
Ruby
300μm
Diamond

## Slide 8: Pressure medium supplements
There is a pressure medium.
Similar to a theoretical situation.
For XRD(X-ray diffraction)
Gas: Helium
Liquid: Mixture of the alcohol.
For electric resistance measurement.
Solid: NaCl
There is no pressure medium.
Similar to a real situation.
Pressure intensity
Diamond cullet
Having medium
No medium

## Slide 9: Experimental method supplements
  X-ray diffraction(XRD)
For the accurate measurement of c/a ratio.
Three runs
Sample: Be (purity 99.5%)
Pressure medium: He
Method: single crystal XRD
Diamond anvil cell
Imaging plate
(検出器)
X-ray
Waves intensified by interference satisfies the Bragg’s condition is observed
X-ray is diffracted by electron.
干渉
Bragg’s condition
2dsinθ=nλ
c
a

## Slide 10: Difficulty of the experiment of Be
The peak intensity of Be is weak.
There is low atomic number of Be.
It’s difficult to load Be in diamond- anvil cell.
Be is so hard and toxic.
Sample size is too small.
X-ray diffraction patterns@~40GPa
Integrated X-ray diffraction patterns
Hole diameter is 100μm
300μm

## Slide 11: P-V and c/a of Be Experiment
Beryllium contained in He or NaCl medium(pressure medium).
Beryllium remained hcp up to the maximum pressure.(205GPa)
The scatter of the c/a ratio is smallest for the current data.

## Slide 12: Summary
The c/a ratio has been took with the highest precision.
No sign of β-Be has been observed at moderate pressure. The stability field of β-Be would be much narrower than previously thought.

## Slide 13: Future work
The enhancement of Tc under high pressure is reported in recent research. According to that the Tc has relation to the drop of c/a ratio.
I will experiment to inspect the c/a ratio of beryllium under high pressure at SPring-8.
Sorry, the data is under analyzing.
I’ll show it you next presentation.
THE END.