## Slide 1
Master Colloquium
Field-effect Control of Insulator-metal Transition Property in Strongly Correlated (La,Pr,Ca)MnO3 Film
Ion Liquid (IL)
LPCMO channel
Electric Double Layer Transistor
TANAKA LAB.
Takuro Nakamura
Gate
Source
Drain
Working as p-type
1

## Slide 2: Metal Insulator Transition (MIT) in 3d Transition Metal Oxide Materials
Electron Crystal
Electron Liquid
External field
Strongly correlated electron materials
have strong Coulomb interaction between narrow 3d-orbitals
Gigantic physical properties changes emerge from electronic phases transition
2

## Slide 3: (La1-x-yPryCax)MnO3
La,Pr,Ca
Mn
O
(La, Pr, Ca) MnO3
3+
3+
2+
3+/4+
Mn3+
(d4)
Mn3+
(d4)
eg
t2g
Mn3+
(d4)
Mn3+
(d4)
Mn4+
(d4)
Mn3+
(d4)
eg
t2g
Mn3+
(d4)
Mn3+
(d4)
LaMnO3
3+
3+
Mn4+
(d4)
Mn3+
(d4)
eg
t2g
Mn3+
(d4)
Mn3+
(d4)
Insulator
Metal
3

## Slide 4: (La1-x-yPryCax)MnO3
0.35
Low T
High T
Nature 399 560 (1999)
PRB 51, 14103 (1995)
La1-xSrxMnO3
4
La,Pr,Ca
Mn
O

## Slide 5: Conventional Field-effect-transistor
Insulator
Source
Gate
Drain
p-type semiconductor
VG = 0
VG > 0
Strongly correlated materials are different from semiconductor materials
MISFET
n+
n+
Inversion Layer
VD
ID
VG
5

## Slide 6: Required Carrier for Electric-field-effect
Nature 4241015 (2003)
Carrier 1014 – 1015 cm-2 is required
6

## Slide 7
MOTIVATION
Base experiments for realization of electric-field-effect nano-device
*Fabrication of EDLT structure on LPCMO thin film
*Verification of gate control of electronic properties
Gate
Ion Liquid (IL)
LPCMO channel
Electric Double Layer Transistor (EDLT)
Carrier doping with ionic liquid gating
EDL
Electric field > 1 MV/cm
Capacitance ~10 mF/cm2
7

## Slide 8
Epitaxial LPCMO thin film
Deposited (La0.525Pr0.1Ca0.375)MnO3 on MgO(001) sub. by pulsed laser deposition method.
TSub. = 700 (oC), PO2 = 30 (Pa)
in-situ annealing TSub. = 700 (oC), PO2 = 1000 (Pa)
Out-of-plane XRD
002 MgO
001 MgO
040 LPCMO
// [001]MgO
Target
ArF excimer laser
(l =193 nm)
Substrate
Thin film
Heater
Plume
Pluse Laser Deposition
t = 20 nm
8

## Slide 9
Fabrication Process of LPCMO-channel EDLT
MgO (001) substrate
Depositing LPCMO film
Depositing Au/Ni electrode
hall-bar structure
Sputtering
SiO2 seperator
Putting ionic liquid
(DEME-TFSI)
9

## Slide 10
LPCMO-channel EDLT structure
Ionic liquid
DEME-TFSI
Source
Drain
20 mm
LPCMO thin film thickness : ~ 8 nm
Gate
Vds = 0.1 V , VG = -3~+3 V applied at 220K
Sweep 220~10 K and measure Resistivity
Picture of EDLT
200 mm
11

## Slide 11
(La, Pr, Ca) MnO3
3+
3+
2+
3+/4+
Mn4+
(d3)
Mn3+
(d4)
eg
t2g
Mn3+
(d4)
Gate voltage dependence of the transport properties
in LPCMO Thin Film
Verified LPCMO thin film work as p-type with Electric-field-effect
S
D
20 mm
t = 8 nm
11

## Slide 12
Insulator
Metal
Nano-scale Phase Separation
COI
FMM
(La,Pr,Ca)MnO3 thin film
TMI
12

## Slide 13: Nano-scale Phase Separation
COI
FMM
Science 285, 1540 (1999)
FMM
COI
200nm
(La,Pr,Ca)MnO3 thin film
Phase separation picture
Coexisting FerroMagnetic Metal (FMM)
and Charge Ordered Insulator (COI)
with nano-meters scale
TMI
13

## Slide 14
VG ＜ 0 [V] (hole doping) FMM rich
VG = 0 [V]
VG ＞ 0 [V] (electron doping)
COI rich
Tuning volume fraction of metal domain and insulator domain
by electrostatic carrier doping
Origin of Resistivity Changes with EDL Gating
Metal
Insulator
T ~ TMI
14

## Slide 15
Summary & Future Work
Gate
Ion Liquid (IL)
Oxide channel
MgO
LPCMO
300nm
LPCMO nano-wire
*I succeed to fabricate EDLT structure
*I verified field-effect resistivity change in LPCMO
Work as p-type
*fabricating EDLT structure
on the LPCMO nano-wire
15