## Slide 1: Fiber-coupled microsphere laser
Ashida lab M1 toyota
M. Cai, O.Painter, K. J. Vahala, Opt. Lett. 25, 1430 (2000).

## Slide 2: Image

## Slide 3: Contents
Introduction
・Laser
・Microsphere resonator
・Mode number
・WGM spectra
・Coupling (fiber-taper , microsphere)
Sample
Results
・Photoluminescence spectra
・Laser power
・Bisphere system
Summary

## Slide 4: Laser
Cavity (resonator)
Laser medium
E
E
Population inversion
Stimulated emission
hν

## Slide 5: Resonator
Q-factor
Mode volume
large (high)
small (low)
reflection loss

## Slide 6: Microsphere resonator
Whispering gallery modes !!
Geometric optics
Wave optics
High Q-factor despite small mode volume

## Slide 7: Whispering gallery modes
Mode number n,m,l
Fundamental WGM → n = 1
l = 4
l = 3
half wavelength

## Slide 8: Whispering gallery modes
m = 0
m = l － 2
m = l
m = 0
m = l － 2
m = l

## Slide 9: Spectra
Wavelength
Wavelength
Oblate sphere
sphere
l = 2
l = 3
l = 4
l = 2
l = 3
l = 4
intensity
intensity

## Slide 10: Coupling (fiber-taper , microsphere)
Resonance of Evanescent light
Total reflection

## Slide 11: Sample
Phosphate glass
・Yb 20 %
・Er 0.5 %
Transformation temperature
・450 ℃
Refractive index
・1.521 (at 1.5 μm)
E
1.5 μm
coupling
Absorption
976±5 nm
α = 4~5
Non-radiative
decay

## Slide 12: Set up
pump wave
spectrometer
microsphere resonator

## Slide 13: Photoluminescence spectra
Pump wave
…980 nm
Sphere
…57 μm
Taper
…1.75 μm
Main
Absorbed pump power
≈120 μW
Output laser power
≈1 μW
Inset
Absorbed pump power
≈200 μW
Output laser power
≈2.6 μW

## Slide 14: Laser power
Lasing threshold = 60 μW

## Slide 15: Bisphere system

## Slide 16: Summary
Fiber-coupled microsphere laser
Single sphere
・lasing threshold is estimated at 60 μW
・single mode …. Max 3 μW
Bisphere
・first laser …. 1535 nm
・second laser …. 1533 nm

## Slide 17: Future plan

## Slide 18: WGM spectra
Leinonen, J., Python code for calculating Mie scattering from single- and dual-layered spheres. Available at http://code.google.com/p/pymiecoated/.

## Slide 19: Mode number
l
m
n
Zoom in
About mode number l,m,n
Tobias Jan August Kippenberg, Nonlinear Optics in Ultra-high-Q
Whispering-Gallery Optical Microcavities, Ph.D. thesis, California Institute of Technology,(2004).
x
y
z

## Slide 20
l = 4
n = 1
n = 2

## Slide 21: Fabry-Perot filter
θ
mλ＝2 top cosθ
top