## Slide 1: Theoretical Studies in Material Dependence of in Cuprate Superconductors
H.Sakakibara et al., PRB-85, 064501 (2012)
H.Sakakibara et al., PRB-89, 224505 (2014)
MORISHITA Naoki
Kusakabe laboratory M1
Division of Frontier Materials Science, Department of Material Engineering Science
Graduate School of Engineering Science, Osaka University

## Slide 2: Contents
Introduction
  Superconductivity and superconductors
Theoretical models and approaches
  Conventional Modeling: The Single-orbital Model
  New Modeling : The Two-orbital model
  Sakakibara’s Rule
Summary

## Slide 3: Superconductivity &
Superconductivity(S.C.)
– the critical temperature
Material with high- is desirable!
Introduction
Phenomena
・zero resistivity
・Meissner effect
・pinning effect
・Josephson effect
Temperature（K）
Resistivity（Ω）
Applications
・power line
・linear motor train
・NMR/MRI
・SQUID

## Slide 4: Cuprate Superconductors
A group of materials that shows high
The structures and variety
Introduction
Cu plane(s)
Block layer(s)
Buffer layer(s)

## Slide 5: Material Dependence of
Records of
How do we approach these materials theoretically?
Introduction
liquid nitrogen
temperature
77(K)↓
30(K)
(1986)
90(K)
(1987)
135(K)
(1993)
153(K)
(under high-pressure)
(2013)
166(K)!?
(under high-pressure)
(2005)
http://sakaki.issp.u-tokyo.ac.jp/user/kittaka/contents/others/tc-history.html

## Slide 6: Conventional Modeling
The single-orbital model
Considering only Wannier orbital
Theoretical models and approaches
Wannierized wave function
Whole structure on the Cu-O plane
  Conventional Modeling

## Slide 7: Conventional Modeling
The Hubbard model(single-orbital)
Theoretical models and approaches
:Coulomb interaction on a site
:Nearest neighbor hopping
:Second nearest neighbor
hopping
:Third nearest neighbor
hopping
0.15 holes per site = optimal doping(最適ドープ)
  Conventional Modeling
We know much about superconductivity of this model.

## Slide 8: 𝑟 and 𝜆
: measure of the
Fermi surface warping
(フェルミ面の曲がり具合)
(: small→good nesting, large →bad nesting)
: the eigenvalue of the
Eliashberg equation
for -wave S.C.
Theoretical models and approaches
H.Sakakibara et al., PRB-85, 064501 (2012)
:r=0.14
:r=0.37
→
If the modeling were proper, should correspond to real .
  Conventional Modeling

## Slide 9: Comparison with Experiments
Theoretical models and approaches
The single-orbital model that takes account of
Cu- orbital ALONE is insufficient here.
So, let us move on to a better model.
◆:Theory
(single-orbital model)
●:Experimentally
observed
H.Sakakibara et al.,
PRB- 89, 224505(2014)
25
75
100
50
●
●
  Conventional Modeling

## Slide 10: New Modeling
The two-orbital model
  Two Wannierized wave functions
  Let be the energy level offset
  between and Wannier orbitals.
Theoretical models and approaches
= +
New Modeling
+
H.Sakakibara et al.,
PRB-85, 064501 (2012)
small
large
Each compound has its .

## Slide 11: Modeling of the system
Two-orbital model
Theoretical models and approaches
per site, holes per Cu atom
:Intra orbital repulsion(軌道内の反発)
:Nearest neighbor hopping
:Second nearest neighbor
hopping
:Third nearest neighbor
hopping
:Inter orbital repulsion(軌道間の反発)
:Hund’s coupling
:Pair-hopping interaction
Bad for S.C. ／(^o^)＼
Good for S.C.＼(^o^)／
New Modeling

## Slide 12: , vs. E
The plots of theoretically
obtained and
both shows a positive
correlation between
, and .
The discussion can be
applied to single-layer
and multi-layer cuprates.
Theoretical models and approaches
H.Sakakibara et al.,PRB- 89, 224505(2014)
→ dominates
both and !
New Modeling

## Slide 13: Comparison with experiments
Thus theoretically obtained correlation between
and is compatible with experimental results!
Theoretical models and approaches
H.Sakakibara et al.,PRB- 89, 224505(2014)
◆:
●:
■:
□:
■:
(a)Theory
(b)Experiment
※
for two-layer cuprates
New Modeling

## Slide 14: Sakakibara’s rule
Dr. Sakakibara proposed a new rule in material dependence of : a cuprate that has large and small is good for superconductivity.
→ We call this as “Sakakibara’s rule”.
With the rule, we can newly design such materials that display high-.
Theoretical models and approaches
 | Existing high- cuprates | Our aim
 | Large(→large !) | Large(→large !)
 | Large(→bad nesting…) | Small(→good nesting!)
 |  | Our aim
 | Large(→bad nesting…) | Small(→good nesting!)

## Slide 15: Summary
In the discussions in cuprate superconductors, the two-orbital model is compatible with the results of experiments but the single-orbital model is not.
With appropriate modeling, Dr. Sakakibara obtained a rule in cuprate superconductors:
large E and small is good for superconductivity.
We can apply the rule to material design for high- cuprate superconductors.
Thank you for your kind attention!

## Slide 16: MEMO