## Slide 1: Ultrabroadband spectroscopy in photo-excited semiconductors
[1]Masaya Nagai, Makoto Kuwata-Gonokami.
Journal of Luminescence 100 (2002) 233-242
Tomohide Morimoto ,ashida lab.

## Slide 2: Luminescence in photo-excited semiconductors
Semiconductor emission devise is important for present photonics
Wikipedia LED
http://www.ccsinc.co.jp
Even now, the spectral analysis of the emission is not established
  Many-body effects for e-h pairs
  Strong Coulomb interaction in wide-gap semiconductors

## Slide 3: exciton, biexciton, and e-h plasma in semiconductors
exciton, biexciton
electron-hole plasma
e-h pair is analogous to hydrogen atom
Ex. hydrogen atom, hydrogen molecule, plasma
(solid) , gas, liquid
e-h density
insulator
metallic

## Slide 4: Many-body effects for e-h plasma(1)
(
V
r
)
r
0
r
/
1
µ
r
e
r
/
k
-
µ
Screening of Coulomb potential causes Bandgap shrinkage

## Slide 5: Many-body effects for e-h plasma(2)
In the emission processes of e-h pairs, it is not clear whether k-conservation rules can be applied.
me
mh
E’g
hn
E’g
me
mh
+
hn
k

## Slide 6: Interband transition and intraband motion
Interband transition
Strong Coulomb interaction
Spectral overlap
Photon mediated effects
Changes of e at low energy side is
caused by intra-band free carrier motion.
M
e
t
a
l
l
i
c
I
n
s
u
l
a
t
o
r
p
h
o
n
o
n
e
x
c
i
t
o
n
b
a
n
d
g
a
p
R
e
f
l
e
c
t
i
v
i
t
y
m
i
d
-
I
R
f
a
r
-
I
R
n
e
a
r
-
I
R
U
V
V
i
s
.
1
0
E
m
i
s
s
i
o
n
w

## Slide 7: Plasma reflection
w
R
w<wp
e<0 → R~1
Simple assumption of uniform plasma
distribution can explain this.
Energy(eV)
wavelength(µm)

## Slide 8: Example: CuCl e-h system
CuCl I-VII compound semiconductor
Eg=3.395 eV
Large exciton binding energy, Eex=213 meV
Stable biexciton

## Slide 9: Time-integrated emission spectrum
+
-
+
-
+
-
ω
emission
+
-
+
-
+
-
+
-
+
-
+
-
+
-
+
-
ω
emission
What’s this?

## Slide 10: Time-resolved emission spectrum
Continuous change of EHP emission
to Stable EHP or biexciton ?
405
400
395
390
15ps
3ps
10ps
Notes: 先に左下の説明

## Slide 11: Transient reflectivity in mid-IR region
Increase of reflectivity shows ionization of e-h pairs
Simple assumption of uniform plasma distribution cannot explain this

## Slide 12: Spatially condensed plasma
D
R
/
R
0
R
0
+
D
R
6
5
4
3
2
1
0
-1
1
2
3
4
5
6
7
8
9
10
Wavelength (µm)
1.0
0.8
0.6
0.4
0.2
0.0
0.1
2
3
4
5
6
7
8
9
1
Energy (eV)
0.2
0.0
1
0
-1
1 ps
10 ps
20 ps
4.1 mJ/cm
2
CuCl 8K
383nm ex.
0.9 mJ/cm
2
5 ps
R
e
f
l
e
c
t
i
v
i
t
y
w
P
1
0
p
l
a
s
m
a
m
e
t
a
l
l
i
c
c
o
l
l
o
i
d
Metallic colloid is formed

## Slide 13: Summary
In addition to the emission spectra, this paper measure transient reflection in mid-infrared after the intense ultrashort pulse excitation in CuCl to get the complementary information for the interpretation of the luminescence
In results, this paper conclude that unknown emission called X-band is attributed to metallic colloid.

## Slide 14: My work
THz-time-domain-spectroscopy
＋
Broadband coherent detection
Ultrashort pulse by hollow fiber
p
h
o
n
o
n
e
x
c
i
t
o
n
b
a
n
d
g
a
p
R
e
f
l
e
c
t
i
v
i
t
y
m
i
d
-
I
R
f
a
r
-
I
R
n
e
a
r
-
I
R
U
V
V
i
s
.
1
0
w

## Slide 15
e
-
e
e
-
e
f
M
M
e
f
f
2
e
M
+
e
e
f
f
=
1
-
f
M
(
)
b
e
f
f
2
e
b
+
e
e
f
f
+
0
f
M
<
<
1
metallic colloid