## Slide 1: High pressure study on superconductor KxFe2-ySe2
M1 Hidenori Fujita
Shimizu group

## Slide 2
Introduction
  Iron based superconductor
  KxFe2-ySe2
Experiment
  Methods
  Result & Discussion
Conclusion
Contents

## Slide 3
Introduction
Iron based superconductor
Simple structure ⇒ easy to analyze
K Deguchi et al.
Sci. Technol. Adv. Mater. 13 054303 (2012)
http://sakaki.issp.u-tokyo.ac.jp/user/kittaka/contents/others/tc-history.html

## Slide 4
Pressure enhances two SC-phase
Tc of second phase is 48 K higher than first phase.
Introduction
KxFe2-ySe2: two dome of SC-phase
L. Sun et al. Nature 483, 67 (2012).

## Slide 5
Introduction
KxFe2-ySe2: Phase separation
There are two coexisting phase mesoscopically: superconducting phase and insulating phase
Chen et al. PRB 86, 184511 (2012)
A. Ricci et al., Supercond. Sci. Technol., 24, 082002 (2011).
122-type
245-type
Fe
Fe-vacancy

## Slide 6
Making method = flux method
Quenching has effects on physics property: electric resistance, magnetic moment, …
Electric resistance:
Quenching temperature when the sample grows is high
⇒ hump shape appears
⇒ metallic behavior
Introduction
KxFe2-ySe2: Effect of quenching
Zhou et al. arXiv:1401.6906 (2014)
Fei Han et al. Philosophical Magazine 92 2553-2562 (2012)

## Slide 7
Pressure effect on KxFe2-ySe2
Introduction
J. Guo et al. PRL 108, 197001 (2012)
122-type
245-type
The hump is suppressed and shifted by pressure
  The hump disappear at 10 GPa
Around 10 GPa, the peak of Fe-vacancy-ordered phase also disappear

## Slide 8
Motivation
To research the SC-2 phase in some materials
  Quenching effects
  Degree of Fe vacancy and K (their composition)
Introduction

## Slide 9
Experiment
Pressure device: Diamond anvil Cell
Measurement: temperature dependence of electric resistance

## Slide 10
Samples
Restore in Ar gas
Experiment
Sample 3
K0.62Fe1.65Se2
Slow cooling
Meissner effect was not observed
Sample 2
Quench at 400℃
Meissner effect was observed at 32 K
Sample 1
K0.77Fe1.68Se2
Quench at 550 ℃
Meissner effect was observed at 31 K.

## Slide 11
Previous result: quenched at 550℃
Result

## Slide 12
Previous result: quenched at 400℃
Result

## Slide 13
Recent result: slow cooling
Result
At 12 GPa, we observed two transition

## Slide 14
Diagram of Tc vs P
Result
metal

## Slide 15
Three type samples show same pressure dependence of Tc under the 10 GPa.
  Quenching temperature doesn’t have effect on SC1-Phase
Over 10 GPa, there are some differences among these samples
  Quenching may compress the SC2-phase. Slow cooling seems better to emerge SC2-phase.
Conclusion

## Slide 16
Future work
Research the repeatability.
  Plan to measure the sample cleaved from previous crystals.
Measure the resistance at higher pressure
  Plan to apply pressure up to 20 GPa.
Measure the new sample
  The sample quenched at 700℃
Conclusion

## Slide 17
Possibility of time dependence
Problems
First run
second run
Third run

## Slide 19
研究背景

## Slide 20
研究背景

## Slide 21
研究背景

## Slide 22
Introduction
Iron based superconductor: pnictide and chalcogenide
Chalcogenide = compound with 16th periodic family (O, S, Se, Te)
Pnictide = compound with 16th periodic family (N, P, As, Sb)
Many iron based superconductors are pnictide
In 122-type structure, chalcogenides seems to be better in Tc
Dong et al. PRL 104, 087005 (2010)
Guo et al. PRB 82, 180520 (2010)
Temperature dependence of electric resistance of KFe2As2
Temperature dependence of electric resistance of KFe2Se2
Notes: IBSC have two type, those are chalcogenides and pnictide.
Chalcogenide = compound with 16th periodic family like this
Pnictide = compound with 16th periodic family like this
Mainly, IBSCs are pnictide. A IBSC which show highest Tc in IBSC is also pnictide. However recently chalcogenides also show high Tc, so these materials get attention in term of the origin of SC

## Slide 23
Bao et al. Chin. Phys. Lett. 30, 027402.(2013)
Basic structure is 122-type structure.
Fe-vacancy have two state: ordered and disordered state.
  Fe-vacancy-ordered makes 245-type structure
122-type = superconductor
245-type = insulator
Introduction
KxFe2-ySe2: structure
122-type
245-type
vacancy
a-axis
Shoemaker et al. PRB 86, 184511 (2012)
Notes: The difference between the phases is a state of Fe-vacancy-order. Basically KxFe2-ySe2 is 122-type structure, which is tetragonal layer structure. When potassium is doped, iron atoms are removed. Then the positions of Fe-vacancies can be ordered or disordered. Ordered state makes 245-type structurein which iron vacancies make superstructure square root of 5, and disordered state is 122-type structure. In a previous slide, the insulator phase show this vacancy-order with TEM. So these phases coexist like this.
As I show, SC is emerged by disorder phase, but on the other hand, it is wondered whether the 245-type structure has any relation or not.
熱処理を加えた試料との測定がこちらになりますが、この測定から鉄の 価のスペクトルが大きくなっていることが確認されています。ここから、熱処理により超伝導相が大きくなっていることがわかります。
これらのことから現在では完全に金属相のみの試料を作成し、超伝導の発現と相分離が関連するかが調べられている。

## Slide 24
Metal transition
  Around 10 GPa, there is certain transition.
  The pressure region corresponds to metal transition.
Result
Notes: これらの試料において共通してみられるのは10GPaでの電気抵抗の振る舞いの大きな変化です。このように金属化がみられています。そのほかの研究でも欠陥のオーダーがなくなり金属化が観測されています。

## Slide 25
Introduction
KxFe2-ySe2:
how to make the sample
Self flux method: making the crystal by using flux.
Mixing substance and flux
Heating and fluxing
Recrystallize
Notes: This phase separation seems to be affected by quenching. many papers report effects on physics properties like electric resistance. This figure show the effect. Each measurement have different heat treatment. Not annealing, ……. As you see, when quenching temperature raises, temperature dependence of resistance changes. At 300 degrees Celsius, the hump shape appear like this.
この物質にはアニールと急冷により超伝導などの物理特性が変化することが知られています。電気抵抗の変化についてもさまざまな研究が行われており、急冷の温度が低いと絶縁体的、高くなるにつれ超伝導が現れ、hungがみられる。急冷時の温度が高温になるにつれ、高温側にシフトしていくことが知られています。
このhungがなくなると超伝導が確認できなくなることが知られています。このことから超伝導とこのhungの関連に興味が持たれています。