## Slide 1
Nanoscale imaging and control of resistance
switching in VO2 at room temperature
Jeehoon Kim, Changhyun Ko, Alex Frenzel, Shriram Ramanathan,
and Jennifer E. Hoffman
APPLIED PHYSICS LETTERS 96, 213106 (2010)
Tanaka lab.
Kotaro Sakai

## Slide 2
Contents
・Introduction
Strongly correlated electron system
The characteristics of VO2
Domain structure in VO2
・Experiment
Methods
Result & Discussion
・Summary
・Future work

## Slide 3
Band Width : wide
Band Width : narrow
Partial occupation ⇒
Metal
Partial occupation ⇒ but Insulator
Coulomb's repulsion U
Strongly correlated electron system
Stimulation
Temperature
Electric field
Magnetic field
Light

## Slide 4
High-T: metal
Low-T: insulator
Science 318, 1750 (2007)
The characteristics of VO2

## Slide 5
Domain configuration
10nm
[001]
[110]
VO2
TiO2
TiO2
VO2
crack

## Slide 6
・Transmittance
・Work function
Appl. Phys. Lett. 101, 191605 (2012)
Insulator
Metal + Insulator
Metal
・Seebeck coefficient
Nano Lett. 9, 4001(2009)
・Carrier density
Phys. Rev. B 79, 153107 (2009)
Appl. Phys. Lett. 102, 153106(2013)
The characteristics of VO2

## Slide 7
Nature Nanotech. 7, 723 (2012)
Domain boundary

## Slide 8
n=4
・Step resistivity changes in 200nm VO2 wire on Al2O3(0001)
50nm
Domain size ＝ 50nm～
Appl. Phys. Lett. 104, 023104 (2014)
Nano domain in VO2

## Slide 9
・VO2
Thickness : 200 nm
Rms roughtness : ～ 6 nm
・Si substrate (As-doped)
Resistivity : 0.002-0.005 Ωcm
Sample details

## Slide 10
Measurement system
grain
on Al2O3 or Si
（Volmer-Weber growth mode)
VO2
n-type Si
I

## Slide 11
Transition by applied voltage
VO2
n-type Si
I
VO2
n-type Si
I
・They succeeded to demonstrate a threshold switching
by Joule heating.
P=100μW

## Slide 12
500nm
Domain mapping
I
・The insulating state displays variations
in conductivity up to 100%.
・Conductivity appears lower in the grain boundary.
Current (μA)

## Slide 13
500nm
Domain mapping
・The metallic state nucleates at the grain
with largest insulating-state conductivity

## Slide 14
Domain mapping
Current (μA)
・Lower conductivity grain boundaries remain
apparent as well as the insulating phase.

## Slide 15
Summary
・They demonstrated a threshold switching by using
metal-insulator transition in a single domain of VO2.
・This transition results most directly from
Joule heating.
・Conductivity appears lower in the grain boundaries
due to a different stoichiometric phase.

## Slide 16
Future work
10nm
[001]
[110]
VO2
TiO2
TiO2
VO2
crack
・・・・・・・・・・・・・・・・・・・・・・・
・・・・・・・・・・・・・・・・・・・・・・・
・・・・・・・・・・・・・・・・・
on TiO2
（Frank van der Merwe growth mode)
grain
on Al2O3 or Si
（Volmer-Weber growth mode)
No crack & grain boundary

## Slide 17
Future work
Nb-dope TiO2
A cantilever coated with Pt or Rh
I
Sample stage (Cu)
Science 318, 1750 (2007)

## Slide 18
Future work
Insulator
Metal
Pt coated tip
TiO2 substrate
Pt
I
L
500nm
VO2 nano-wire
Pt
Pt
300μm
20μm
AFM image
Pt
Pt
VO2 nanowire
50nm

## Slide 20
crystal | VO2 | TiO2 | Al2O3
Lattice constant (nm) | 0.455 | 0.459 | 0.476
Lattice mismatch(%) | - | 0.863 | 4.41
Lattice mismatch

## Slide 21
Temperature[K]
Resistance[Ω]
VO2-VO2
VO2-TiO2(Nb dope)
z
・
・
・
・
VO2
Nb-dope TiO2substrate
R-T curve on Nb doped TiO2