## Slide 1: Observation of ultrafast nonlinear response due to coherent coupling between light and confined excitons in a ZnO crystalline film
Ashida Lab.
Subaru Saeki

## Slide 2: Contents
Introduction
Background
Coherent coupling between light and confined excitons
Degenerate four-wave mixing (DFWM)
Previous work
Comparison between ZnO and GaN
Motivation
Sample
Experimental setup
Results
Summary
Future work

## Slide 3: Background (Realization of optical router)
Optical router light → light
Electronic router light → electrical signal → light
Transient grating
Signal light
Merit
Noise is reduced.
Energy efficiency can be improved.
Transmission speed increases.
Control light

## Slide 4: Background (Realization of optical router)
Requirement for optical router
→ High efficiency and high-speed response
10 ps order
(exciton lifetime : 100ps～)
Trade-off problem!
 | efficiency | speed
resonance | ○ | ×
non-resonance | × | ○
Processes associated with the exciton resonance cause high efficient optical response.
High-speed response in resonance process is required!

## Slide 5: Coherent coupling between light and confined excitons
The n=1 exciton dominantly interacts with light.
n = 4
n = 3
n = 2
n = 1
Both efficiency and speed of response is enhanced with increase of system size,
but saturated in larger region
Multinode-type excitons complicatedly interact with light.
Both efficiency and speed of optical response are size-resonantly enhanced.
Nanostructure
Long wavelength approximation region
System where exciton wave functions are
coherently extended to the whole volume

## Slide 6: Degenerate four-wave mixing (DFWM)
Two-pulse configuration
Probe pulse
Pump pulse
Non-linear medium
Transient grating (TG)
DFWM signal
Probe pulse
Pump pulses
Non-linear medium
Transient grating (TG)
TG signal
The decay profile is determined by population and phase relaxations
The decay profile is determined by only population relaxation
Three-pulse (TG) configuration

## Slide 7: Previous work 1 (CuCl high-quality films)
Appearance of peculiar spectrum structures
Ref: M. Ichimiya, M. Ashida, H. Yasuda, H.Ishihara and T. Itoh, Phys. Rev. Lett. 103, 257401 (2009)
Ultrafast radiative decay of 100 fs order
DFWM spectrum

## Slide 8
A,B exciton resonance energy
EA:3.376eV
EB:3.381eV
Previous work 2 (ZnO)
Enhancement of radiative width by coupling between A and B excitons
T. kinoshita, H. Ishihara, JPS 2014 spring meeting, 27aCD-13.
Thickness (nm)
Eigenenergy (eV)
Radiative width (meV)

## Slide 9: Previous work 3 (ZnO)
ZnO thin film with the thickness where an excitonic state shows ultrafast decay time
Optical nonlinearity is also enhanced at the same thickness.
n=1
n=2
n=3
n=4
n=5
Thickness (nm)
Radiative decay time(fs)
Integral intensity of non-linear response (Optical kerr)
Larger nonlinearity and faster radiative decay than CuCl is expected.
T.kinoshita, H.Ishihara, JPS 2014 spring meeting, 27aCD-13.

## Slide 10: Comparison between ZnO and GaN
ZnO and GaN have attracted attention as wide band gap semiconductor.
 | ZnO | GaN
Room temperature band gap (eV) | ～3.37 | ～3.4
Exciton binding energy (meV) | ～60 | ～28
Exciton Bohr radius (nm) | ～1.4 | ～3.2
electron
hole
polarization
Binding energy =
Stability of exciton
Band structure of ZnO
In terms of stock quantity, stability of exciton and safety,
ZnO is superior to GaN.
ZnO is expected as blue light-emitting devices, optoelectronic devices etc.
Notes: Gaはレアメタルと呼ばれ、日本はリサイクルを除くと、そのすべてを中国、台湾、カザフスタンなどからの輸入に頼っている。2050年までの需要量が埋蔵量の6倍と予測されている。供給不足の可能性が考えられる。
それに比べてZnはベースメタルと呼ばれ、社会で大量に使用され、生産量が多い。

## Slide 11: Motivation
Observation of ultrafast radiative decay in CuCl crystalline films
Observation of ultrafast and highly efficient nonlinear response due to coherent coupling between light and confined excitons in a ZnO crystalline film
Possibility of enhancement of non-linearity
Application possibility for optical devices
ZnO

## Slide 12: Sample (ZnO)
Pulse laser deposition (PLD) method
Thickness : 330nm
Substrate : Al2O3 (0001)
Providing source：
Osaka city university Nakayama lab.

## Slide 13: Experimental setup (TG configuration)
Mode-locked
Ti:Sapphire
laser
Parabolic mirror
Polarized beam splitter
Spectroscope
BS
SHG crystal
Cryostat
Optical delay stage
Pulse width : 110 fs
Repetition frequency : 80 MHz
λ/2 wave plate
5 K～

## Slide 14: DFWM spectrum (two pulse configuration)
Reflection spectrum shows sharp peak structures in the exciton resonance region.
EA EB
Two peaks appear at the energy region lower than the exciton resonance energy.
Reflection of high crystalline quality
Effect of coherent coupling between light and confined excitons
DFWM signal
DFWM
Reflection
:
3.378 eV Exc.

## Slide 15: DFWM spectrum by TG method
Three peaks are observed.
Spectral widths reflect the radiative widths for the corresponding excitonic states.
The radiative decay times are estimated by the value of Γ.
Pump
Probe
TG signal
= (Γ：radiative widths)
Eigenenergy (eV) | 3.3585 | 3.3655 | 3.3699
Spectral width(meV) | 12.1 | 4.26 | 3.11
Radiative decay time(fs) | 54 | 154 | 211
Eigenenergy (eV) | 3.3585 | 3.3655 | 3.3699
 | 12.1 | 4.26 | 3.11
 | 54 | 154 | 211

## Slide 16: Radiative decay profile of excitons (by TG method)
Ultrafast radiative decay times in the order of 100 fs are observed.
The decay times agree well with the calculated values estimated by spectral widths.
Pump
Probe
TG signal
Delay time

## Slide 17: Summary
In a ZnO crystalline film, peculiar spectrum structures due to coherent coupling between light and confined excitons are observed.
In TG spectrum, peculiar spectral feature with three peaks is observed, and the radiative decay time of each excitonic state is estimated from the spectral width.
Ultrafast radiative decay in the order of 100 fs is observed, and the decay times agree well with the values estimated by spectral widths.

## Slide 18: Future plan
Comparison of radiative decay time with other excitonic states
Observation of DFWM signal and the decay profile at room temperature
Estimation of optical nonlinearity by measuring nonlinear refractive index using optical kerr effect
Comparison with other materials (CuCl, GaN, ZnSe, anthracene)

## Slide 19: Back ground (Optical communication)
optical fiber
Optical communication use higher five figures frequency than electric communication.
Ultrafast pulsed light of 6fs (electronic circuit : ~0.1ns)
Optical signal
Optical signal