## Slide 1: Investigation of fluid- fluid phase transition of hydrogen under high pressure and high temperature
2014/11/26
Shimizu laboratory
SHO Kawaguchi

## Slide 2
Contents
Introduction
  Hydrogen under high pressure
  Previous work
My study
  Experimental method
  Results
Summary & Future work

## Slide 3
Introduction
Solid metal and superconductor under ultra high pressure (P > 400 GPa) → very difficult
Fluid metal under high pressure and high temperature

## Slide 4
Introduction
Aurora of Jupiter
Cross section of Jupiter
JAXA
Metallic - liquid hydrogen circulate in Jupiter
→ Strong magnetic field
JAXA

## Slide 5
Previous work
W. J. Nellis, S. T. Weir, and A. C. Mitchell, Phys. Rev. B 59, 3434 (1999)
Shock wave experiment
Metallization
P = 140 GPa,
T < 3000K

## Slide 6
Previous work
M. A. Morales et al., PNAS, 107, 29, 12799-12803(2010)
from insulator to metal
Theoretical calculation

## Slide 7
Heating efficiency changes
Phase transition
Change of thermal conductivity
Change of Reflectance
Heat of transition etc.
LASER power
Temperature
Phase
transition
transition temperature
Previous work
Temperature vs LASER Power
Plateau
sample
Heating LASER
LASER heating

## Slide 8
Previous work
V. Dzyabura et al. PNAS, 110, 20, 8040-8044 (2013)
Heating efficiency changes
→ phase transition
Heating LASER (Palse)
LASER heating
Plateau

## Slide 9
Motivation
Generating metallic liquid hydrogen under hydrostatic pressure
Investigation of boundary between Insulator Liquid and Metallic Liquid

## Slide 10
Experiment
・Sample : H2
・Anvil Culet : φ100 or 150 μm
・Gasket : Re
・LASER absorber : Au
・Pressure determination method
: Diamond Raman
Re Gasket
Diamond Anvil Cell (DAC)

## Slide 11
Experiment
High diffusibility
  → Hydrogen embrittlement of diamond anvil
  Hydrogenation of Rhenium gasket
High compressibility
  → Contraction of the sample room
Technical difficulties of experiments
Apply pressure
@ 50 GPa
@ 1 atm

## Slide 12
Experiment
Sample room formed by FIB (FIB = Focused Ion Beam)
Formation of the sample room using FIB
  → to prevent the diffusion of hydrogen
NaCl wall on the inner wall of gasket
    to prevent hydrogenation of the gasket
Ti-coating on diamond surface
    to prevent Hydrogen embrittlement of diamond anvil
→
→
NaCl

## Slide 13
Experimental
IR LASER
Laser Heating @SPring-8/BL10XU
・Heating LASER : 1053 nm fiber LASER
・Temperature Determination method
: radiation measurement
・ XRD before and after heating
  To comfirm that Au and NaCl don’t react
・ Raman spectroscopy before and after heating
  To comfirm that Hydrogen remains

## Slide 14
Results
Temperature vs LASER Power
Heating efficiency changes

## Slide 15
Results
No changing point
Without hydrogen
Control experiment
No Hydrogen
Hydrogen

## Slide 16
Results
No changes of X-ray pattern of Au and NaCl
XRD patterns before and after heating
H2 vibron before and after heating
Hydrogen remained after heating

## Slide 17
Heating efficiency changes
→ Thermal conductivity and
reflectance change
→ Phase transition
LASER power
Temperature
Phase
transition
transition temperature
Results
Temperature vs LASER Power

## Slide 18
Results
Phase diagram of Hydrogen
Critical point

## Slide 19
Summary
In the LASER heating experiment, heating efficiency changes
On the other hand, heating efficiency doesn’t change without hydrogen
These results shows good agreement with theoretical calculations
The transition was observed
above critical point by
theoretical calculation
Critical point

## Slide 20
Future work
In order to confirm the metallization directly….
Electric resistance measurement
  Drop of electric resistance with the metallization
  However, insulating gasket is difficult to confine the hydrogen
  → Optimization of the insulation layer
shrinking
Before filling
After filling