## Slide 1: Pressure dependence of crystal structure and superconductivity in beryllium
2014.11.26
Shimizu Lab.
M1 Takuya Yamauchi

## Slide 2: Contents
Introduction
Superconductivity of light elements
Enhancement of Tc
Structure
Previous work
Motivation
Experiment
Measurement of X-ray diffraction.
Measurement of electrical resistance.
Result＆Discussion
Summary

## Slide 3: Superconductivity of light elements Introduction
My target
Ref. HP@SPring8(2011)
The superconducting critical temperature(Tc) of beryllium is very lower than other light elements.
Beryllium
Tc=24mK

## Slide 4: In case of Calcium and Lithium
0.4 mK
Tc of Li < 0.4 mK at 1 atm, but under high pressure, Tc ~16 K.
Ref. T. Matsuoka, et al., j, phys, 121, 052003 (2008).
Ref. M. Sakata., et al., PRB 83, 220512 (2011).
Calcium’s Tc achieves 29 K, which is the highest Tc in elements.
Calcium
Lithium
29 K
16 K

## Slide 5: Enhancement of Tc Introduction
In BCS theory
Tc = 1.14 θD exp [ -1 / N V ]
θD: Debye temperature
N: Density of state at the Fermi surface
V: Interaction between electron and lattice vibration
θD of Be is 1440 K.
In light elements
Intensity of attraction between the electron does not change that causes increase of ωd.
ωd : Debye frequency
Tc ∝ θD, N,V
very high
θD
cf. Li 344 K
Ca 230 K
However
Tc(24 mK) is too low.
Approaching to N,V
Applying pressure

## Slide 6: Structure of beryllium Introduction
Beryllium has small c/a ratio.→ 1.568
(Its ideal value of hcp is 1.633 )
hcp(～1530 K)
bcc(1530～1560 K)
Melting point: 1551 K
heat
pressure
hcp structure is
stable at ambient temperature and pressure.
bcc structure would be appeared at high temperature and prssure.
Ref. D. A. Young, Phase Diagrams of the Elements (University of California, 1991), P. 79.c

## Slide 7: Previous work Introduction
Ref. K.Kubota修士論文(2013)
The Tc of beryllium has enhanced in a pressure range, where a decrease its c/a ratio was observed.
No pressure medium

## Slide 8: Motivation
Diamond anvil cell
Imaging plate
(検出器)
X-ray
1. I’ll confirm whether the structure changes.
→ measure the c/a ratio and volume by using powder X-ray diffraction.
2. I’ll measure the electrical resistance of beryllium to see the its drop caused by superconductivity.
Ref. K.Kubota 修士論文(2013)
The decrease of electrical resistance rate is only 0.13%.
Experiment @Spring-8 BL10XU

## Slide 9: Settings Experiment
For the accurate measurement of c/a ratio.
Sample: Be (99.9 %)
Diamond anvil: 300 μm
Gasket: Re
Pressure marker: Ruby
Pressure medium: none, He(gas)
sample
Gasket
Pressure maker
300μm
Diamond anvil
Beryllium
Ruby
once twice
NM
He
: No pressure Medium
: with pressure medium He
NM
He
静水圧
非静水圧

## Slide 10: X-ray diffraction pattern Experiment
The peak 002 disappeared with applying pressure.
λ=0.413Å
λ=0.414Å
Beryllium’s atomic number is 4, so it has very few electrons.
NM
He
Beryllium has characteristic five peaks.
Affection of orientation is weak.
配向

## Slide 11: Orientation Experiment
配向
a
c
My sample beryllium is polycrystal.
a
c
: Direction of the crystal
NM
Peak corresponding to c-axis is weakened.
pressure

## Slide 12: Calculation of c/a ratio Experiment
Bragg’s condition
2dsinθ=λ
d=
λ=0.414Å
const.
Miller index | (100) | (002) | (101) | (102) | (110)
Low pressure | 〇 | 〇 | 〇 | ○ | 〇
High pressure | 〇 | × | 〇 | × | 〇
Calculate with the cellcalc.
The value of c/a ratio can have more error at high pressure.
100
002
101
102
110
He

## Slide 13: c/a ratio Result＆Discussion
[1] K.Kubota 修士論文(2013)
with pressure medium He
The c/a ratio increase monotonically with
increasing pressure.
No pressure medium
The c/a ratio decrease at specific pressure.
c/a vs P
He
NM

## Slide 14: Setting Experiment
For the measurement of electrical resistance.
Sample: Be (99.9 %)
Diamond anvil: 300 μm
Gasket: SUS310S
Insulator layer: c-BN with epoxy
Electrodes: Pt
Pressure medium: none
Pressure marker: Ruby
Gasket
ruby
Insulator layer
Electrodes
sample
Pressure maker
11.2 GPa
31.2 GPa
300μm
NM

## Slide 15: Electrical resistance Result＆Discussion
R vs T
Low temp.
NM

## Slide 16: Problems Result＆Discussion
Possibility
Pressure effect.
Impurities(Fe)
Setting.
Oxidization of sample.
Error of data.
Its decrease is only 0.05 mΩ

## Slide 17: Summary
I confirmed the changes of c/a ratio in beryllium.
The changes have caused by presence or absence of pressure medium.
The decrease of electrical resistance caused by superconductivity couldn’t be seen.
THE END.

## Slide 18: ρvsT @room temp.
Chart: ρvsP
| 10 | 15 | 19 | 24 | 26 | 30 | 34 | 38
K.Kubota | 43.3333 | 62.7 | 80 | 97.0667 | 120.4 | 155 | 252 | 336.6667
My data | 34.5 | 29.25 | 30.2 | 27.475 | 22.95 | 18.125 | 16.625 | 17 | 18.625 | 19.5 | 20.75 | 20.75 | 18.625

## Slide 19: Difference of setting
Before sampling
38 GPa
Previous work
My work
Before sampling
31 GPa
ρ