## Slide 1: NMR study on bismuth oxide superconductor BaPbxBi1-xO3
H. Matsuura and K. Miyake, J. Phys. Soc. Jpn. 81 (2012) 113705
Kitaoka Lab.
Takashi MATSUMURA
K.Kumagai.et,al Physica C 274 (1997) 209-220

## Slide 2: Contents
Introduction
NMR,NQR
Result
137Ba spectrum
137Ba・135Ba T1
Summary

## Slide 3
TCmax~30K
Ba1-XKXBiO3
1988
spin
Spin
+
orbital
phonon
BaPbXBi1-XO3
Tcmax~12K
1975
History of Superconductors
Introduction
Valence skipper?

## Slide 4
O
(1s)2(2s)2(2p)4
O2-
(1s)2(2s)2(2p)6
Bi
[Xe](4f)14(5d)10(6s)2(6p)3
Bi3+
Bi5+
[Xe](4f)14(5d)10(6s)2(6p)0
[Xe](4f)14(5d)10(6s)0(6p)0
Skipping (ns)1 state
Valence skipper
結晶化学入門 遠藤忠 他
講談社サイエンティフィック、wikipedia
Valence skipper
Introduction
Anion
Cation
closed-shell structure
stable structure
Bi4+
[Xe](4f)14(5d)10(6s)1(6p)0
unstable structure

## Slide 5: Negative U
Introduction
6s0
6s1
6s2
: Energy of electron
US: Coulomb interaction
<E1
Attraction
US<0

## Slide 6: Candidates for Valence skipper SC
Introduction
Valence skipping effect?
Nb1-xTaxSe3 (Nb3+,Nb5+)
AgSnSe2 (Sn2+,Sn4+)
Pb1-xTlxTe (Tl1+,Tl3+)
BKBO,BPBO (Bi3+,Bi5+)
-Na0.33V2O3 (V3+,V5+)
・
・
・
・
・
・

## Slide 7: Mother compound BaBiO3
Perovskite structure
BaPbxBi1-xO3
Different valence Bi

## Slide 8: Mother compound BaBiO3
/
BaPbxBi1-xO3

## Slide 9: Superconductivity of BaPbxBi1-xO3
BaPbxBi1-xO3
sc
BaBiO3
Bi
[Xe](4f)14(5d)10(6s)2(6p)3
Pb
[Xe](4f)14(5d)10(6s)2(6p)2
Hole doping
BaPb0.5Bi0.5O3
BaPbO3
Hole doping
CDW state
CDW state

## Slide 10: Samples
sc
Hole doping
BaPbxBi1-xO3
x=0.64 Semiconductor
x=0.75 Superconductor
x=0.91 Metallic
0.64
0.91
BaBiO3
CDW state
BaPbxBi1-xO3

## Slide 11
Ex. I=1/2
I=1/2
H0＝0
H0≠0
m=+1/2
m=-1/2
gℏ H0
Zeemann splitting
ω= g H0
NMR (Nuclear Magnetic Resonance) 核磁気共鳴
γ (gyromagnetic ratio) 磁気回転比
Nuclear Magnetic Resonance
Zeeman interaction
NMR,NQR
NMR Intensity [a.u.]
Frequency,H0
ω,H0

## Slide 12
NMR,NQR
NQR Intensity [a.u.]
Frequency
Nuclear Quadrupole Resonance
Ex. Ba I=3/2
+
+
+
+
m=±1/2
m=±3/2
hνQ
quadrupole interaction

## Slide 13
137Ba NQR Spectrum of x=0.91: Metallic
=13MHz
=10.9, 1
(T=1.6K)
Spectrum

## Slide 14
Nuclear Magnetic Resonance
Ex. Ba I=3/2
NMR,NQR
=9MHz
ω~42MHz
NMR Intensity
=0.4
=0
ω
EFG:電荷分布
Real, broadening
Ideal
=1
Real, broadening
Ideal
ω

## Slide 15: Mother compound BaBiO3
Perovskite structure
BaPbxBi1-xO3
Rotation

## Slide 16
Ba site: tetragonal
0
1
Spectrum
(1,0,0)
VXX
VXX
VZZ
VZZ
VYY
VYY

## Slide 17
Spectrum
0
1
Ba site: orthorhombic
1 : tetragonal
1 : orthorhombic
Crystal structure  Spectrum shape

## Slide 18
137Ba NMR Spectrum of x=0.91: Metallic
x=0.91
Metallic
=10.9
1
Spectrum
20K
One component
tetragonal

## Slide 19
137Ba NQR Spectrum of x=0.64: Semiconductor
=12.5MHz,14MHz
=10.9, =0.9
=12.5, =0.65
(T=1.6K)
two two
Spectrum

## Slide 20
137Ba NMR Spectrum of x=0.64: Semiconductor
=12.5
= 0.65
=10.9
=0.9
40%
60%
+
=10.9
=0.9
=12.5
= 0.65
Spectrum
20K
Two components
tetragonal
orthorhombic

## Slide 21
Two components
=14.3
= 0.4
=11.5
=0.8
30%
70%
+
=11.5
=0.8
=14.3
= 0.4
137Ba NMR Spectrum of x=0.75: Superconductor
Spectrum
20K
tetragonal
orthorhombic

## Slide 22
(1)
(1)
Part of 1
Tetragonal phase
x=0.91 Metallic
x=0.64
Semiconductor
x=0.75
Superconductor
Tetragonal phase
+
Orthorhombic distortion
Temperature vs
Tetragonal phase
+
Orthorhombic distortion
Spectrum
T<350K
T<350K
Whole temperature
Tetra
Tetra
Tetra
Ortho
Ortho

## Slide 23
m=+1/2
m=-1/2
H0
time
t
M
M(t) = M(∞)[1- exp(-t/T1)]
Thermal equilibrium state
M = M（∞）
Relaxation
M = M（t）
Exited state
M = M(0) = 0
t < 0
t = 0
t > 0
0
Ex. I=1/2
Ba T1
Electronic spin, etc.
Nuclear magnetic relaxation rate (T1-1)

## Slide 24
Ba T1
137Ba/135Ba-NMR
T1Q-1
T1M-1
Valence skipping fluctuation?
T1-1=T1M-1+T1Q-1
Nuclear magnetic relaxation rate (T1-1)

## Slide 25
Nuclear magnetic relaxation rate (T1-1)
x=0.91 Metallic
x=0.75 Superconductor
x=0.64 Semiconductor
Ba T1
small
large
Ea

## Slide 26: Samples
sc
Hole doping
BaPbxBi1-xO3
x=0.64 Semiconductor
x=0.75 Superconductor
x=0.91 Metallic
0.64
0.91
BaBiO3
C
D
W
fluctuation
small
large
CDW
fluctuation?
Ba T1

## Slide 27
Pair hopping
Bi
Bi
Bi
Bi
Pb
Pb
Pb
Pb
Pb
Pb
Pb
Pb
Pb
Pb
Pb
Pb
BaPbxBi1-xO3
x=0.75
Pair hopping

## Slide 28
Bi (6S) state
Pair hopping
BaPbxBi1-xO3
x=0.75
Pair hopping

## Slide 29
Bi (6S) state
Pair hopping
BaPbxBi1-xO3
x=0.75
Negative U
Pair hopping

## Slide 30: Summary
Superconductivity and a change of the structure are in a close relation.
Nuclear relaxation mechanism was determined by charge fluctuations.
The superconductivity in BPBO may be mediated by the valence skipping effect.