## Slide 1
Electric-field Effect on Transition Properties in
a Strongly Correlated Electron (La,Pr,Ca)MnO3 Film
Electric Double Layer Transistor
Source
Drain
Gate
Ionic liquid
Takuro Nakamura

## Slide 2
3d transition metal oxide materials
Ti
Ni
V
Co
Cr
Mn
Fe
Cu
Metal-Insulator
transition
VO2
Ferromagnetic
Fe3O4,Fe3-xZnxO4
Ferroelectric
BaTiO3
High temperature
superconduction
YBa2Cu3O7
Various functionalities with the huge response
H. Zheng et al., Science 303 30 (2004).
Y.J. Chang et al., Thin solid films 486 46 (2005).
N. Suzuki et al., small 4 1661 (2008).
J.Z. Sun et al., Phys. Rev. Lett. 58 1574 (1987).

## Slide 3
Mn
O
La+3,Pr+3,Ca+2
(La, Ca) MnO3
3+
2+
3+/4+
Mn3+
(d4)
Mn3+
(d4)
eg
t2g
Mn3+
(d4)
Mn3+
(d4)
Mn4+
(d3)
Mn3+
(d4)
eg
t2g
Mn3+
(d4)
Mn3+
(d4)
LaMnO3
3+
3+
Mn4+
(d3)
Mn3+
(d4)
eg
t2g
Mn3+
(d4)
Mn3+
(d4)
Insulator
Metal
Manganite material : (La1-x-yPryCax)MnO3 (LPCMO)
Major carriers : holes

## Slide 4
Insulator-to-metal transition in LPCMO
TC
Insulator
Metal
La0.275Pr0.35Ca0.375MnO3 film
External field
(T, H, VG)
RI/RM ~104
Gigantic resistance change should be controlled by VG.

## Slide 5
Field effect transistor (FET)
Gate
Source
Drain
Substrate
Gate insulator
Insulator
insulator
Gate control of the number of charge carriers and resulting electronic states.
VG
Metal
Notes: Field effect transistor is enable to control charge carriers by applying external field

## Slide 6
Key component : gate insulator
Q = CV
C = ere0S/d
n = Q/S = ere0V/d
Gate
Source
Drain
Substrate
Gate insulator
Q : electric charge
C : capacitance
Gate insulator

## Slide 7
Large n is needed for phase transition
C. H. Ahn et al., Nature 424, 1018 (2003).

## Slide 8
Field effect transistor Using Ionic liquid
Electric Double Layer
Ionic liquid (molten salt)
E ~ 1 MV/cm
C ~ 10 mF/cm2
n ~ 1013-1015 /cm2
N, N-diethyl-N-methyl-N-(2-methoxyethyl) ammonium bis (trifluoromethanesulfonyl) imide (DEME-TFSI)
Electric Double Layer Transistor (EDLT)
http://www.ekouhou.net

## Slide 9
Typical issue for ionic liquid : electrochemical
*Electrochemical carrier dope
S
D
VG on
Reversible
Irreversible
*Electrostatic carrier dope
S
D
VG off
S
D
VG off
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
h+
×
MOTIVATION
Realizing electrostatic carrier doping in LPCMO-EDLT
*Finding a suitable gate bias range for electrostatic effect
*Transition property modulation using electrostatic effect
Reversible/Irreversible effects depend on gate voltage.
K. Ueno et al., Appl. Phys. Lett. 96 252107 (2010).
H. T. Yi et al., Sci. Rep. 4 6604 (2014).
Reversible is a key for device.

## Slide 10
Pulsed laser deposition : (La0.525Pr0.1Ca0.375)MnO3 / MgO(001) sub.
TSub. = 700oC, PO2 = 30 Pa
in-situ annealing TSub. = 700oC, PO2 = 1000 Pa
Film growth
MgO (001) substrate
Depositing LPCMO film
Depositing Au/Ni electrodes
hall-bar structure
Sputtering
SiO2 separator
Putting ionic liquid
(DEME-TFSI)
EDLT Fabrication
Fabrication process of LPCMO-channel EDLT

## Slide 11
Fabrication process of LPCMO-channel EDLT
Source
Drain
Gate
Ionic liquid DEME-TFSI
VDS = 0.1 V , gate voltage (VG) was applied at 220 K
Pulsed laser deposition : (La0.525Pr0.1Ca0.375)MnO3 / MgO(001) sub.
TSub. = 700oC, PO2 = 30 Pa
in-situ annealing TSub. = 700oC, PO2 = 1000 Pa
Film growth
20 mm
LPCMO film thickness : 8 nm
EDLT fabrication
Transport property investigation

## Slide 12
VG dependent transfer characteristics
Reversible or irreversible
Scan rate : 9×10-2 mV/sec
Reversible/irreversible electric current change appeared depending on the gate voltage.
Iirreversible
Itotal
S
D
VG on
h+
h+
h+
h+
h+
h+
ID
S
D
VG off
Reversible
S
D
VG off
S
D
VG on
h+
h+
h+
h+
h+
h+
Irreversible
1 V
2 V
3 V
220 K

## Slide 13
Field effects induced by Electric-double-layer
Electrostatic effect vs. Electrochemical effect
Electrostatic effect is dominant at VG ≤ 2 V.
Reversible change
Irreversible change

## Slide 14
Gate control of metal-to-insulator transition
Successfully control metal-to-insulator transition with electrostatic effect.
TC
Insulator
Metal
 and Tc at -2V
 and Tc at +1V

## Slide 15
Gate voltage induced carrier accumulation
Mn
O
Major carriers are holes ; p-type
La+3,Pr+3,Ca+2
zero gate bias
(La0.525Pr0.1Ca0.375)MnO3
h+
h+
h+

## Slide 16
Gate voltage induced carrier accumulation
negative gate bias
Mn
O
h+
h+
h+
Negative gate bias dopes more holes into a LPCMO.
La+3,Pr+3,Ca+2
Accumulated holes promote the transition.
h+

## Slide 17
Gate voltage induced carrier accumulation
Mn
O
La+3,Pr+3,Ca+2
Positive gate bias depletes holes in a LPCMO.
Depleted hole discourages the transition.
positive gate bias
h+
h+

## Slide 18
Gate voltage induced carrier accumulation
Mn
O
La+3,Pr+3,Ca+2
Positive gate bias deplete hole in a LPCMO.
Depleted hole discourages the transition.
positive gate bias
h+

## Slide 19
Gate control of transition property
Electrostatic effect realized the modulation of transition property.
increase
decrease
hole
encourage
discourage
I-M transition

## Slide 20
summary
We have fabricated the LPCMO-EDLT structure and investigated the gate effect on its transport property.
Transfer characteristic measurements revealed the reversible electrostatic carrier doping at below a gate voltage 2 V.
We successfully control transition properties with electrostatic carrier doping effect.
Notes: Finally, I’d like to make a brief summary of my work.
,,,,
Thanks for your attention!

## Slide 22
Fabrication of LPCMO film
Pulsed laser deposition : (La0.525Pr0.1Ca0.375)MnO3 / MgO(001) sub.
TSub. = 700oC, PO2 = 30 Pa
in-situ annealing TSub. = 700oC, PO2 = 1000 Pa
Film growth
Target
ArF excimer laser
(l =193 nm)
Substrate
Thin film
Heater
(~1073K)
Plume
Notes: This is a typical LPCMO film channel EDLT.
Then the transport property has been investigated with VDS = 0.1 V , gate voltage (VG) was applied at 220 K.

## Slide 23
Typical issue for EDLT
K. Ueno et al., Appl. Phys. Lett. 96 252107 (2010).
J. Jeong et al., Science 339 1402 (2013).
Reversible
Irreversible
Notes: However, question remains open, This kind of method , we should take into account the electrostatic effect and electrochemical effect like this. In contrast with the electrostatic effect which could be obtain reversible effect, electrochemical effect give rise to irreversible nature. In the previous reports have indicated these two effects depending on gate bias.＋図の説明
In the present work, we have found a gate bias range with electrostatic or electrochemical effects. And then measured electrostatic carrier doping effects in LPCMO-EDLT. What we have done is as follows.

## Slide 24
Phase Separation in manganite
FMM
COI
200nm
M. Uehara et al., Nature 399 560 (1999).
Electronic phase separation between in COI (charge-ordered insulator) and FMM (ferromagnetic metal) in a sub-micrometer scale has been observed.
Phase separation is important to decide material properties.
L. Zhang et al., Science 298 805 (2002).

## Slide 25
A model considering phase separation
to describe IMT quantitatively
2s
Domain : 50×50
r0=358.3, a=3.88×10-2, b=4.38×10-8
c=0.118, Eg=1.31×10-4 [eV/K]
s = 17 K
TC = 173 K
Metal
Coexist
Insulator
Metal
Insulator
Determing of s and TC

## Slide 26
Gate control of phase separation
-2V
0 V
+1V
-2V@100 K
+1V@100 K
0V@100 K
8 nm-(La0.525Pr0.1Ca0.375)MnO3
Metal
Insulator